**HUNTEX NIS-11**

**SOFTENER**

**General trait**

1. Appearance : Milky white to milky yellow paste
2. Ingredient : Aliphatic quaternary compound.
3. pH : 5.0 ±1.0 (25oC, 1% aqueous solution)
4. Ionicity : Cationic.
5. Solubility : Can disperse completely in cold water

**Characteristics**

1. Gives woven fabric a soft, smooth and full hand feeling to a variety of fabrics and yarns.
2. This product is cationic softener with the very low yellowing, the whiteness of the textiles are affected very little.

**Application**

The product is useful in applications as softener for cotton, synthetic fabrics, apparel in washing workshops.

**Usage**

**NIS-11** can be applied to the textiles by dipping, exhausting and padding. The suitable treating temperature is about 50°c.

1. Exhaust method, recommended dosage : 1.0% 🡪 5.0% o.w.f
2. Pad method, using amount : 5.0g/l 🡪 50g/l

**Package**

120 kg/barrel